## Slide 1: Magnetic diffraction: Exploring hidden magnetic symmetries
Johan Cedervall
johan.cedervall@mmk.su.se

## Slide 2: Magnetic materials

## Slide 3: Neutron diffraction
X-rays
Small samples
Strong absorption
High energy (1 Å = 12.4 keV)
Low penetration depth
Light elements hard to detect
Scattering power highly Q dependent
Neighbouring elements cannot be discriminated
High availability (lab)
Cannot distinguish isotopes
Magnetic structures not easily probed
Neutrons
Large samples
Low absorption
Low energy (1 Å = 81.81 meV)
High penetration depth
Light elements can be seen
Scattering power almost Q independent
Neighbouring elements can be discriminated
Low availability (large scale fac)
Isotopes can be distinguished
Magnetic structures easily probed

## Slide 4: Magnetic diffraction
MnO2
Itot = Inuclear + Imagnetic
For ferromagnetic structures the magnetic unit cell equals the nuclear unit cell and there are extra magnetic contributions to the intensities of the reflections
For antiferromagnetic structures the magnetic unit cell is often larger than the nuclear one and there are extra pure magnetic reflections

## Slide 5: Magnetic diffraction
Magnetic space groups
Similar to conventional space groups
Adds a parameter to relay the magnetic moment behavior
Compare
  Pnma
  Pn’m’a
1651 different magnetic space groups
Irreproducible representations
Symmetries are divided into the smallest possible representation (Γ)
Analysis is performed and only symmetry representations that are relevant are considered
Can build up complex models without space group restrictions

## Slide 6: Magnetic diffraction
For all magnetic structure solution attempts other input parameters are needed:
Magnetic measurements
Crystallographic information
k-vector

## Slide 7: Science examples

## Slide 8: Fe2P
Hexagonal compound,
Ferromagnetic
Studied for its magnetocaloric properties, which are tuneable with substitutions to Fe1-xMnxP1-ySiy
TC = 220 K

## Slide 9: Fe2P
Measurements conducted at IN5@ILL
J. Cedervall et al. Physical Review B 99 (2019) 174437

## Slide 10: Fe2P
Integrated intensity of (1 0 0) and (0 0 1) suggests a canting of the magnetic moments above(!) TC
Also shown from magnetic structure refinements
Supported from Mössbauer spectroscopy
J. Cedervall et al. Physical Review B 99 (2019) 174437

## Slide 11: Fe2P – magnetic structure solution
k-vector = (000) and ferromagnetic
Combining two irreproducible representations gives a solution for the magnetic moment in the ac-plane
J. Cedervall et al. Physical Review B 99 (2019) 174437

## Slide 12: Fe2P – magnetic structure solution
New measurements were performed using the beamline Polaris@ISIS with ambition of analyzing the magnetic short range order using mPDF
Magnetic models from IN5 could not be reproduced
  Magnetic space groups were analyzed instead
Supports only directions along c, or ab

## Slide 13: Fe2P – magnetic structure solution
The space groups and were both tested
Similar, indistinguishable magnetic structure solutions

## Slide 14: Fe2P - summary
Canting close to TC is observed using both irreps. and magnetic space groups
Magnetic moments are comparable to magnetometry results independent of magnetic structure model
Magnetic space group models suggest that one of the iron sites in the structure loses its magnetic moment before the other
  Has been previously suggested by DFT calculations E. K. Delczeg-Czirjak et al. Physical Review B 82 (2010) 085103
To fully resolve the magnetic structure, single crystal neutron diffraction must be employed
  Requires big(!) samples

## Slide 15: Mn3M20X6
Cr23C6-type structure, S.G.
Can adopt plenty of elements on both M and X sites
Magnetic and structural properties determined on both intermixing on the metal positions as well as the distances between the magnetic atoms
Mn3Ni20P6 and Mn3Co20B6 will be illustrated here

## Slide 16: Mn3Ni20P6
Mn3Pd20P6 is ferromagnetic
T. Eriksson, et al. Journal of Magnetism and Magnetic Materials 308 (2007) 203-209
Substitutions of Pd to Ni gives a more complex magnetization curve
Only difference is the Mn-Mn distance

## Slide 17: Complex magnetism in Mn3Ni20P6
3 magnetic transitions
= 3 magnetic structures
at 30, 26 and below 20 K
J. Cedervall et al. Journal of Solid State Chemistry 237 (2016) 343–348

## Slide 18: Complex magnetism in Mn3Ni20P6
30 K
26 K
J. Cedervall et al. Journal of Solid State Chemistry 237 (2016) 343–348

## Slide 19: Complex magnetism in Mn3Ni20P6
30 K
26 K
<20 K
J. Cedervall et al. Journal of Solid State Chemistry 237 (2016) 343–348

## Slide 20: Ferromagnetism in Mn3Co20B6?
Possibly stronger magnetic interactions compared to Mn3Ni20P6 given the stronger magnetic element Co
Magnetomtry suggests a ferromagnetic ground state stable from TC at 540 K down to 4 K
S.R. Larsen et al. Unpublished

## Slide 21: Ferromagnetism in Mn3Co20B6?
Crystallographic information?
700 K
Mixed metal occupancies!
S.R. Larsen et al. Unpublished

## Slide 22: Ferromagnetism in Mn3Co20B6?
k-vector = (0 0 0)
6 K
S.R. Larsen et al. Unpublished

## Slide 23: Ferromagnetism in Mn3Co20B6?
Magnetic space groups
S.R. Larsen et al. Unpublished

## Slide 24: Ferromagnetism in Mn3Co20B6?
3 different magnetic structure models describe the data equally well
Ferrimagnetic!
Single crystals would solve the problem
S.R. Larsen et al. Unpublished

## Slide 25: Mn3M20X6 - summary
Atomic distances and intermixing of occupancies strongly interacts with the magnetic properties
Type of atoms important
Hard to distinguish similar structures using powder diffraction data

## Slide 26: Summary
Magnetic structures are not easy to determine
Three essential input parameters when solving magnetic structures
  Magnetic measurements
  Crystallographic information
  k-vector
Irreps or MSGs?
  Two ways of describing the same thing
  Complementarity between them
Detrimental for a complete understanding of the physics in the studied material
Magnetic structures are just the beginning!

## Slide 27: Acknowledgements